We hereby guarantee that the following is precise and accurate.

Commodity   :  TRIMETHYLOL PROPANE (TMP)

Chemical formula : C2H5C(CH2OH)3

| Test Item | Specification |
| --- | --- |
| Appearance | White crystal (=White Flake) |
| TMP content (%) | No less than 99.5 |
| Molecular Weight | 134.18 |
| Melting Point (℃) | No less than 58.0 |
| Hydroxyl Group(wt%) | No less than 37.5 |
| Acidity(wt% as formic acid) | 0.02 or less |
| Water content(wt%) | 0.05 or less |
| Ash content (wt%) | 0.001 or less |
| Phthalic Acid Color Scale | 3 or less |
| Specific Gravity (30℃) | 1.1628 |
| Boiling Point (℃) | 292 (30mmHg) |
| Freezing Point (℃) | 61 |
| Flash Point (℃) | 176 |
| Ignition Temperature (℃) | 375 |
| Dust Explosion:Lower Explosive Limit | No data |
| Minimum Ignition Energy | No data |
| Solubility | Ready soluble in water, alcholand and acetone |
| Stability & Reactivety | Stable |
| Name of Classification | Classification standard not applicable |
| Hazardous | Not specially hazardous |
| Harmful | Not specially harmful |